SUPPLEMENTAL INFORMATION

In vitro intestinal toxicity of commercially available spray disinfectant products advertised to contain colloidal silver

Kim R. Rogers1*, Taylor E. Henson2, Jana Navratilova1, Mark Surette1, Michael F. Hughes2,

Karen D. Bradham1, Aleksandr B. Stefaniak3, Alycia K. Knepp3 and Lauren Bowers3

1Watershed and Ecosystem Characterization Division, Center for Environmental Measurement and Modeling, USEPA, RTP, NC 27711

2Methods and Characterization Division, Center for Environmental Measurement and Modeling, USEPA, RTP, NC 27711

3National Institute for Occupational Safety and Health, Morgantown, WV

*Corresponding author: 109 T.W. Alexander Drive, U.S. EPA, Research Triangle Park, NC 27711, United States, Telephone: +1-919-541-3086; Email: rogers.kim@epa.gov

Table S-1. Characteristics of Colloidal Silver Product Suspensions

____________________________________________________________

Product		pH			Cl- (ppm)		S (ppm)

____________________________________________________________

1		6.6			BDL			27.9

2		7.9			39.8			40.4

3		10.6			25.1			BDL

4		10.0			25.3			BDL

5		2.5			10.6			9.8

____________________________________________________________

BDL Below Detection Limit

Table S-2. Estimated Total Ag Doses from Recommended Product Use

Product		Product Application 	Total Measured Ag	Recommended Dose	Dose/Day			(External, Internal)	(mg/L)			(mL)			(ug Ag)

___________________________________________________________________________________

1		Internal			18.9			0.4			7.6

2		Both			961			1			961

3		External		6.0			Light Spray		ND

4		External		6.1			Light Spray		ND

5		External		8.7			Hard Surface Spray	ND

___________________________________________________________________________________

ND Not Determined

A

B

Figure S-1 TEM Images and EDS False Color Images. Product 2 (A) without exposure to SSF or (B) with exposure to SSF. Red represents Ag, green represents Cl.