Supplementary material

Fabrication and Optimization of a Hybrid 3D-Printed Flexible Electrochemical Biosensor for Sensitive Detection of 1-Hydroxypyrene Glucuronide, an Associated Wildfire Exposure Biomarker

Yonghao Fu a,b, Chuchu Chen a, Xinyi Li a, Yang Song a, Christopher D. Simpson c, Luke P. Naeher d

Kaiyan Qiu a, *, Dan Du a, b, *

a School of Mechanical and Materials Engineering, Washington State University, Pullman, Washington 99164, United States

b Department of Pharmaceutical Sciences, College of Pharmacy and Pharmaceutical Sciences, Washington State University, Spokane, Washington 99202, United States

c Department of Environmental & Occupational Health Sciences, University of Washington, Seattle, Washington 98195, United States

d Department of Environmental Health Science, University of Georgia, Athens, Georgia 30602, United States

* Corresponding authors.

E-mail: kaiyan.qiu@wsu.edu; annie.du@wsu.edu

Table of Contents

Figure S1: The cyclic voltammetry curves of the working electrode after different treatments, recorded in a 5 mM [Fe(CN)6]4-/3- solution with 0.1 M KCl as the supporting electrolyte at a scan rate of 50 mV/s.

Figure S2: Signal current response of the 3D-printed flexible electrochemical 1-OHPG biosensor after storage at 4 °C.

Movie S1: Immobilization of hapten-bovine serum albumin conjugate on the working electrode via direct ink writing.

Figure S1. The cyclic voltammetry curves of the working electrode after different treatments, recorded in a 5 mM [Fe(CN)6]4-/3- solution with 0.1 M KCl as the supporting electrolyte at a scan rate of 50 mV/s. The treatments include DMF for 10 min, NaOH for 60 min, H2SO4 for 180 min, and combined treatment using all three solutions.

Figure S2. Signal current response of the 3D-printed flexible electrochemical 1-OHPG biosensor after storage at 4 °C. Measurements were performed using a 5 ng/mL 1-OHPG sample. Signal retention was calculated as It/I0 × 100%, where It is the current after storage time t and I0 is the initial current on day 0. The signal retentions were 99.14%, 97.11%, 96.58%, 94.27% and 91.26% after 1, 3, 5, 7 and 14 days of storage, respectively.