**Supplemental Information**

**Size Distribution and Estimated Respiratory Deposition of Total Chromium, Hexavalent Chromium, Manganese and Nickel in Gas Metal Arc Welding Fume Aerosols**

Lorenzo G. Cena, William P. Chisholm, Michael J. Keane, Amy Cumpston, and Bean T. Chen

**Table S1.** Mass concentration and mass percentage of total concentration of Mn, Cr, Ni and Cr(VI) fumes by size range.

|  |  |
| --- | --- |
|  | Mass concentration (μg/m3) and mass percentage in specified size ranges (μm) |
| *Mild Steel* | <0.01 | 0.01-0.02 | 0.02-0.03 | 0.03-0.06 | 0.06-0.1 | 0.1-0.2 | 0.2-0.3 | 0.3-0.6 | 0.6-1 | 1-2 | 2-3 | 3-6 | 6-10 | 10-20 | >20 |
| *Mn* |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mass conc. | 0.27 | 0.01 | 0.17 | 0.18 | 10.8 | 31.4 | 108 | 99.2 | 21.2 | 6.90 | 1.94 | 1.03 | 0.21 | 0.15 | 0.10 |
|  SD  | 0.21 | 0.01 | 0.06 | 0.07 | 2.86 | 9.31 | 24.3 | 6.01 | 8.10 | 4.05 | 0.63 | 0.38 | 0.09 | 0.10 | 0.09 |
|  Mass % | 0.03 | 0.00 | 0.02 | 0.02 | 3.89 | 11.3 | 38.3 | 35.3 | 7.47 | 2.43 | 0.69 | 0.37 | 0.07 | 0.05 | 0.03 |
|  SD | 0.02 | 0.00 | 0.01 | 0.01 | 1.22 | 3.91 | 7.62 | 2.87 | 2.60 | 1.34 | 0.21 | 0.15 | 0.03 | 0.03 | 0.03 |
|  | Mass concentration (μg/m3) and mass percentage in specified size ranges (μm) |
| *Stainless Steel* <0.01 | 0.01-0.02 | 0.02-0.03 | 0.03-0.06 | 0.06-0.1 | 0.1-0.2 | 0.2-0.3 | 0.3-0.6 | 0.6-1 | 1-2 | 2-3 | 3-6 | 6-10 | 10-20 | >20 |
| *Cr* |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  Mass conc. | 2.15 | 2.35 | 2.83 | 3.03 | 5.92 | 25.2 | 83.4 | 34.5 | 9.42 | 5.20 | 2.55 | 1.78 | 1.17 | 1.10 | 1.54 |
|  SD | 0.45 | 1.18 | 1.39 | 1.89 | 1.37 | 7.84 | 11.2 | 4.99 | 2.26 | 0.47 | 0.47 | 0.82 | 0.87 | 0.80 | 0.88 |
|  Mass % | 0.41 | 0.46 | 0.56 | 0.60 | 3.36 | 14.2 | 47.6 | 19.7 | 5.33 | 2.99 | 1.47 | 1.05 | 0.70 | 0.66 | 0.93 |
|  SD | 0.06 | 0.24 | 0.33 | 0.38 | 0.48 | 2.81 | 2.66 | 1.03 | 0.91 | 0.29 | 0.34 | 0.51 | 0.50 | 0.46 | 0.57 |
|  *Mn* |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  Mass conc. | <0.03 | <0.03 | <0.03 | 0.04 | 7.80 | 37.5 | 114 | 71.5 | 24.0 | 10.2 | 2.06 | 0.91 | 0.20 | 0.08 | 0.17 |
|  SD | - | - | - | 0.08 | 2.14 | 16.8 | 23.0 | 29.0 | 14.1 | 4.96 | 0.89 | 0.20 | 0.17 | 0.11 | 0.30 |
|  Mass % | - | - | - | 0.01 | 2.94 | 13.8 | 43.5 | 26.3 | 8.56 | 3.66 | 0.76 | 0.35 | 0.07 | 0.03 | 0.0 |
|  SD | - | - | - | 0.01 | 0.30 | 2.71 | 4.60 | 5.76 | 2.51 | 0.67 | 0.15 | 0.07 | 0.05 | 0.04 | 0.15 |
|  *Ni* |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  Mass conc. | 0.65 | 0.20 | 0.02 | 0.11 | 1.45 | 6.82 | 21.3 | 7.86 | 2.16 | 1.13 | 0.45 | 0.35 | 0.18 | 0.17 | 0.08 |
|  SD | 1.12 | 0.24 | 0.03 | 0.13 | 0.39 | 1.32 | 2.76 | 0.72 | 0.65 | 0.27 | 0.29 | 0.40 | 0.29 | 0.22 | 0.09 |
|  Mass % | 0.46 | 0.16 | 0.01 | 0.08 | 3.43 | 16.1 | 50.5 | 18.7 | 5.08 | 2.66 | 1.04 | 0.79 | 0.40 | 0.39 | 0.19 |
|  SD | 0.76 | 0.20 | 0.03 | 0.11 | 0.72 | 1.15 | 1.79 | 1.24 | 1.14 | 0.40 | 0.58 | 0.84 | 0.62 | 0.47 | 0.19 |
| *Cr(VI)* |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  Mass conc. | <0.01 | <0.01 | 0.64 | <0.01 | 0.82 | 2.39 | 4.11 | 1.53 | 0.58 | 0.37 | 0.34 | <0.01 | <0.01 | <0.01 | <0.01 |
|  SD | - | - | 1.28 | - | 0.65 | 1.28 | 0.98 | 1.32 | 0.63 | 0.66 | 0.68 | - | - | - | - |
|  Mass % | - | - | 1.82 | - | 6.61 | 23.3 | 47.9 | 11.9 | 4.16 | 2.34 | 1.92 | - | - | - | - |
|  SD | - | - | 3.65 | - | 4.83 | 3.27 | 21.6 | 8.12 | 3.91 | 3.65 | 3.85 | - | - | - | - |