Supplemental Files– SEM analyses

Untreated Limestone (UL)

| Element composition | Particle (spot) number |
| --- | --- |
| C O Ca | 1 2 3 4 5 6 7 8 9 10 11 12 13 15 16 18 19 20 21 22 23 24 25 26 27 28 29 31 32 33 34 35 36 37 38 39 40 43 44 45 46 47 48 49 50 |
| C O Ca Al Si | 14 |
| C O Ca Fe | 17 |
| C O Ca Si | 30 41 42 |

Treated Limestone (TL)

| Element composition | Particle (spot) number |
| --- | --- |
| C O Ca | 2–50 |
| C O Ca Si | 1 |

Untreated Marble (UM)

| Element composition | Spot number |
| --- | --- |
| C O Ca | 1–50 |

No Si element composition was found in 50 Micro-White 100 particles.

Treated Marble (TM)

| Element composition | Particle (spot) number |
| --- | --- |
| C O Ca | 1 2 3 4 5 6 7 8 9 10 11 12 13 14 15 20 21 22 23 24 25 26 27 28 29 30 31 32 33 34 35 36 37 38 39 40 41 42 43 44 45 46 47 48 49 50 |
| C O Ca Al Si | 16 17 19 |
| C O Ca S Fe | 18 |