Electronic Supplementary Information (ESI)

Facet Effects of Palladium Nanocrystals for Oxygen Reduction in an Ionic Liquid and Sensing Application

Yongan Tang,a Xiaowei Chi,a Shouzhong Zou,b and Xiangqun Zeng*a

aDepartment of Chemistry, Oakland University, Rochester, Michigan 48309, United States

bDepartment of Chemistry, American University, Washington, DC 20016, United States

*Address correspondence to zeng@oakland.edu

Figure S1. Cyclic voltammograms at different scan rate of (A) cubic palladium nanocrystals (B) RD palladium nanocrystals in [Bmpy][NTf2] with 0.01 M ferrocene (third cycle), the electrochemical active surface area for Pd{100} and Pd{110} is 32.49 cm2 and 37.49 cm2, respectively.

.

Figure S2. SEM images of (A) RD, (B) Cubic Pd nanocrystals after 300 °C annealing.

Figure S3. Cyclic voltammograms of palladium nanocrystal electrodes in 0.1 M HClO4 solution after annealing treatment (third cycle), scan rate: 100 mVs-1 (potential vs. RHE).

Figure S4. Cyclic voltammograms of polycrystalline platinum electrodes in (solid) 21% v/v oxygen concentration, (dash) pure nitrogen (third cycle). Scan rate: 0.1 V/s.

Figure S5. Different scan rates of cyclic voltammograms for (A) cubic (B) RD Pd nanocrystals in [Bmpy][NTf2] at  (10%, v/v) oxygen.  Peak current vs. square root of scan rate plots for (C) cubic (D) RD Pd nanocrystal.

Figure S6. Charge ratio of oxygen redox peaks for two types of palladium nanocrystals in [Bmpy][NTf2] obtained in Figure 2A and 2B.

Table S1. The names and structures of ionic liquid and possible deprotonated cation structures

| [NTf2]- |  | [Bmpy]+ |  |
| --- | --- | --- | --- |
| [Bmpy]de+ (1) |  | [Bmpy]de+(2) |  |